Supplementary Information

Landscape of Acetylene Production

Zihao Zhang, Abhinandan Nabera, Gonzalo Guillén-Gosálbez, Javier Pérez-Ramírez*

Institute for Chemical and Bioengineering, Department of Chemistry and Applied Biosciences, ETH Zurich, Vladimir-Prelog-Weg 1, 8093 Zurich, Switzerland.

*Corresponding author. E-mail: jpr@chem.ethz.ch

Table of Contents

Supplementary Notes 1–2

Supplementary Tables 1–5

Supplementary References

Supplementary Note 1

Life cycle assessment methodology

The global average climate change impacts are quantified using an attributional life cycle assessment (LCA) in accordance with the ISO 14044/14040 standards. We consider 1 kg of acetylene (C2H2) produced as the functional unit, following a cradle-to-gate approach that includes all activities from raw material acquisition to C2H2 production. The cradle-to-gate scope assumes that the end-use phase is the same regardless of the synthesis route. The mass and energy flows for the calcium carbide (CaC2), partial combustion (PC), thermal plasma, and non-thermal plasma routes for C2H2 production were obtained from literature, as shown in Supplementary Table 3. This data allows us to model the foreground system (C2H2 production plant), while data for the background system (activities supplying inputs to the production facility) were primarily sourced from the Ecoinvent v3.10 database. We consider the 100-year average global warming potentials (GWPs) as implemented in the IPCC 2021 methodology. The inventories used to calculate the climate change impact for all C2H2 production technologies are shown in Supplementary Table 4.

Furthermore, to calculate the climate change impacts for the year 2050, we performed a prospective LCA. In this context, we considered the most optimistic future scenario for the climate target of 1.5 °C. Therefore, to update the background system, we utilized future projections derived from Integrated Assessment Models (IAMs). IAMs, such as IMAGE (Integrated Model To Assess the Global Environment), provide a holistic understanding of the relationships among the biosphere, society, and the climate. We used the premise v2.1.1 framework to construct future background data aligned with the results obtained from the IMAGE model. Moreover, the IMAGE model assumes particular Shared Socio-economic Pathways (SSPs) that describe the relationship between challenges for adaptation and mitigation. In our study, we assumed SSP2 (“middle-of-the-road”). For the mitigation scenario, we considered the Representative Concentration Pathway (RCP) aimed at limiting the global mean surface temperature to 1.5 °C (RCP19 from premise). All calculations for the environmental assessment were performed using the Brightway2 framework.

Supplementary Note 2

Techno-economic assessment methodology

The mass and energy flows for the CaC2, PC, thermal plasma, and non-thermal plasma routes for the production of C2H2 were obtained from the literature, as shown in Supplementary Table 3. The economic assessment only considers operational expenditures for the reference year 2022. Generally, capital costs are much lower than raw material and utilities consumption expenses; therefore, we neglect capital expenditures, providing a lower bound to the production costs in our analysis. Supplementary Table 5 presents the prices of feedstock and utilities used in the production cost calculations for all the C2H2 production technologies. Unlike the prospective LCA performed in this work, we do not conduct an economic assessment for 2050 due to the significant challenges posed by the high uncertainty and volatility of future energy prices, influenced by geopolitical scenarios and technological improvements.

Supplementary Table 1 Comparison of representative results of thermal and non-thermal (cold and warm) plasma-driven methane coupling processes. Power supply, applied voltage, catalyst type (catal.), conversion, selectivity to C2 products, energy requirement (ER), and specific energy input (SEI) are provided for a direct comparison. aNatural gas is used as the feed in the Hüls arc process. ~: not mentioned; /: not used.

| Plasma type | Power supply/W | Applied voltage/kV | Catal. | Feed | Conv. /% | Selectivity (%) |  |  |  |  | ER/kWh kg−1 C2H2 (SEI/kJ mol-1) | Plasma temp. | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | C2H2 |  | C2H4 |  | C2H6 |  |  |  |
| Hüls arc | 8000k | 81 | / | CH4a | 70.5 | 72.9 |  | 4.5 |  | ~ | 12.1 (275) | thermal | 2 |
| DuPont arc | 9000k | ~ | / | CH4/H2 | 90 | 80 |  | ~ |  | ~ | 8.8 | thermal | 3 |
| low-current arc | 850 | <12 | / | CH4/H2 | 70 | 90 |  | 3.5 |  | <1 | 10.2 | thermal | 4 |
| corona | 8.2 | 10.9 | / | CH4 | 28 | 76 |  | ~ |  | ~ | 26.2 (3403) | cold | 5 |
| corona | 8.4 | 7 | NaY | CH4/H2/O2 | 38 | 32.3 |  | 1.7 |  | 7.1 | ~ | cold | 6 |
| corona | 8.4 | 7 | / | CH4/H2/O2 | 12 | 0 |  | 0 |  | 26 | ~ | cold | 6 |
| pulse corona | 30 | 20-32 | Al2O3 | CH4/CO2 | 43.4 | 22.7 |  | 4.6 |  | 3.3 | ~ | cold | 7 |
| pulse corona | 30 | 20-32 | La2O3/Al2O3 | CH4/CO2 | 24.9 | 54.5 |  | 9.2 |  | 9.1 | ~ | cold | 7 |
| pulse corona | ~ | 18-36 | / | CH4 | 44.6 | 67.5 |  | ~ |  | ~ | ~ (1788) | cold | 8 |
| DBD | 2 | 20 | Fe-MFM-300 | CH4 | 3 | 38 | 58 |  | 0 |  | ~ (44.8) | cold | 9 |
| DBD | 2 | 20 | / | CH4 | 1 | 17 | 47 |  | 22 |  | ~ (44.8) | cold | 9 |
| DBD | 3.3 | 6 | MgO/Al2O3 | CH4 | 23 | 28 | 30.3 |  | 27.4 |  | ~ | cold | 10 |
| DBD | 3.4 | 6 | MgO/Al2O3 | CH4 | 16.2 | 22 | 25.6 |  | 35.5 |  | ~ | cold | 10 |
| DBD | 3.5 | 6 | MgO/Al2O3 | CH4 | 9.5 | 10.5 | 18.6 |  | 48.1 |  | ~ | cold | 10 |
| DBD | 7-8 | 7.6 | / | CH4 | 32 | 6.6 | 5.5 |  | 20 |  | ~ | cold | 11 |
| DBD | 7-8 | 10 | BaTiO3 | CH4 | 5.8 | 18.2 | 31.5 |  | 20.2 |  | ~ | cold | 11 |
| DBD | 7-8 | 9 | γ-Al2O3 | CH4 | 30 | 10.9 | 11.6 |  | 12.9 |  | ~ | cold | 11 |
| DBD | 7-8 | 8.9 | α-Al2O3 | CH4 | 33 | 11.5 | 9.6 |  | 11.5 |  | ~ | cold | 11 |
| DBD | 7-8 | 9.8 | SBA15 | CH4 | 20 | 10.1 | 17.5 |  | 15.2 |  | ~ | cold | 11 |
| DBD | ~ | 17 | / | CH4 | 12.3 | 2.6 | 2.8 |  | 31.2 |  | ~ | cold | 12 |
| DBD | ~ | 17 | 1g Pt/Al2O3 | CH4 | 11.5 | 1.5 | 2.4 |  | 49.1 |  | ~ | cold | 12 |
| DBD | ~ | 17 | 3g Pt/Al2O3 | CH4 | 18.7 | 0.02 | 0.1 |  | 31.4 |  | ~ | cold | 12 |
| DBD | 36 | <30 | Pt/CeO2 | CH4 | 36 | 5.9 | 6.5 |  | 46.6 |  | ~ | cold | 13 |
| DBD | 72 | <30 | Pt/CeO2 | CH4 | 43 | 1.5 | 2.5 |  | 45.1 |  | ~ | cold | 13 |
| DBD | >150 | ~ | TiO2/ZSM-5 | CH4/O2 | 18.4 | 6.5 | 15.7 |  | 8.5 |  | ~ | cold | 14 |
| DBD | >150 | ~ | TiO2/silicalite | CH4/O2 | 8.3 | 10.1 | 16.4 |  | 10.9 |  | ~ | cold | 14 |
| pulsed | 25 | ~ | / | CH4 | 44.3 | 94.6 | 2.8 |  | 0.6 |  | ~ | cold | 15 |
| pulsed | 25 | ~ | / | CH4/O2 | 58.9 | 58.9 | ~ |  | ~ |  | ~ | cold | 15 |
| pulsed | 25 | ~ | / | 1CH4/1H2 | 46.3 | 94.2 | 4.4 |  | 1.1 |  | ~ | cold | 15 |
| pulsed | 25 | ~ | / | 1CH4/9H2 | 11.8 | 63.7 | 15.2 |  | 17.7 |  | ~ | cold | 15 |
| pulsed | ~ | 21 | / | CH4 | 51 | 71.7 | 9 |  |  |  | ~ (250) | cold | 16 |
| pulsed spark | ~ | ~ | / | CH4 | 39 | 83.2 | 3.78 |  | ~ |  | 12.65 | warm | 17 |
| pulsed spark | ~ | 12.3 | / | CH4 | 23.5 | 85.1 | 5.4 |  | 1.9 |  | 9.2 (86) | warm | 18 |
| microwave | 120 | ~ | / | CH4/H2 | 50.7 | 61.4 | 11.5 |  | ~ |  | 73.8 (1076) | warm | 19 |
| microwave | 130 | ~ | Cu | CH4 | 37.7 | 85.9 | 0.5 |  | 2.1 |  | ~ | warm | 20 |
| microwave | 130 | ~ | Cu/W | CH4 | 21.7 | 81.6 | 1.4 |  | 3.2 |  | ~ | warm | 20 |
| microwave | 130 | ~ | Cu/Ni | CH4 | 16.5 | 76.4 | 1.8 |  | 3.6 |  | ~ | warm | 20 |
| microwave | 600 | ~/110 mbar | / | CH4 | 34 | 59 | <2 |  | ~ |  | 24 (224) | warm | 21 |
| microwave | 600 | ~/110 mbar | / | 3CH4/1H2 | 42.7 | 61.8 | <2 |  | ~ |  | 25 (224) | warm | 21 |
| microwave | 600 | ~/110 mbar | / | 1CH4/1H2 | 48.6 | 70 | 2 |  | ~ |  | 28.3 (224) | warm | 21 |
| microwave | 600 | ~/55 mbar | / | CH4 | 31 | 46.2 | 8 |  | ~ |  | 33.2 (224) | warm | 21 |
| microwave | 600 | ~/55 mbar | / | 3CH4/1H2 | 35.5 | 47 | 9.8 |  | ~ |  | 38.5 (224) | warm | 21 |
| microwave | 600 | ~/55 mbar | / | 1CH4/1H2 | 42.1 | 60 | 10 |  | ~ |  | 38.3 (224) | warm | 21 |
| microwave | off | ~ | Mo/ZSM-5 | CH4 | 10.1 | 0 | 14.7 |  | 3.0 |  | ~ | warm | 22 |
| microwave | 110 | ~ | Mo/ZSM-5 | CH4 | 11 | 35.3 | 10.0 |  | 1.9 |  | ~ | warm | 22 |
| microwave | 16 | ~ | / | CH4 | 23.8 | 40.8 | ~ |  | ~ |  | 143 (652) | warm | 23 |
| microwave | 34 | ~ | / | CH4 | 56.6 | 56.6 | ~ |  | ~ |  | 44.7 (674) | warm | 23 |
| microwave | 48 | ~ | / | CH4 | 80.1 | 61.2 | ~ |  | ~ |  | 28.1 (659) | warm | 23 |
| microwave | 70 | ~ | / | CH4 | 94.3 | 71.2 | ~ |  | ~ |  | 20 (627) | warm | 23 |
| microwave | 81 | ~ | / | CH4 | 93.0 | 71.2 | ~ |  | ~ |  | 20.8 (644) | warm | 23 |

Supplementary Table 2 Comparison of representative results of thermal cracking processes with and without catalysts. THN: 1,2,3,4-tetrahydronaphthalen; aHydrogen-permeable tubular membrane reactor

| Temperature/°C | GHSV/ L gcat−1 h−1 (h−1) | Catal. | Feed | Conv./% | Selectivity (%) |  |  |  | Total sel. to C2/% | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | C2H2 |  | C2H4 | C2H6 |  |  |
| 1100 | 24 | Mo2C | CH4 | 23 | 4.8 |  | 12.6 | 3.2 | 20.6 | 24 |
| 1100 | 24 | WC | CH4 | 9.9 | 6 |  | 18.1 | 8.4 | 32.5 | 24 |
| 1000 | 12 | Li/MgO | CH4 | 5 | 0.6 |  | 3.4 | 6.4 | 10.4 | 25 |
| 865 | ~ | FeS2 | CH4/S2 | 7-10 | 1-2 |  | ~ | ~ | 20-37 | 26 |
| 700 | 302 | Mo/ZSM-5 | CH4 | 0.05 | 20 |  | 65 | 5 | 90 | 27 |
| 950 | 6 | CaO-Na-Cl | CH4/CO2 | 18.9 | 9.2 |  | 63.3 | 21.5 | 94 | 28 |
| 950 | 6 | CaO | CH4/CO2 | 9.3 | 4.7 |  | 64 | 31.3 | 100 | 28 |
| 200-1500 | (105) | Pt/Al2O3 | CH4/O2 | 63 | 7-15 |  | 4-5 | <1 | ~ | 29 |
| 925 | 12 | Ni–P/SiO2 | CH4 | 0.8 | 5.9 |  | 63.5 | 17.6 | 87 | 30 |
| 900 | ~ | Ni–P/SiO2 | C2H6 | 100 | 20 | 22 |  | ~ | ~ | 30 |
| 1020 | (9400) | / | CH4 | 5.3 | 17.5 | 27.8 |  | 5.6 | 51 | 31 |
| 1020 | (9400) | cristobalite (CRS) | CH4 | 7.7 | 18.8 | 25.6 |  | 3.8 | 48.2 | 31 |
| 1020 | (9400) | Fe©CRS | CH4 | 6.5 | 19.1 | 27.6 |  | 4.6 | 51.3 | 31 |
| 1020 | (9400) | Fe/CRS | CH4 | 8.1 | 19.1 | 25.1 |  | 3.4 | 47.6 | 31 |
| 1020 | (9400) | Fe-CRS | CH4 | 6.0 | 18.0 | 26.9 |  | 4.9 | 49.9 | 31 |
| 1020 | (9400) | Fe/SiO2 | CH4 | 6.5 | 18.3 | 26.7 |  | 4.6 | 49.5 | 31 |
| 1020 | (9400) | Fe©CRS | CH4/H2 | 5.8 | 29.3 | 53.0 |  | 3.9 | 86.2 | 31 |
| 1020 | 1 | / | CH4 | 3.9 | 11.4 | 27.7 |  | 5.2 | 44.2 | 32 |
| 1020 | 1 | SiO2 | CH4 | 11.3 | 13.2 | 24.9 |  | 1.8 | 39.9 | 32 |
| 1020 | 1 | Fe-SiO2 | CH4 | 8.5 | 14.5 | 29.1 |  | 2.5 | 46.1 | 32 |
| 1020 | 1 | CoFe-SiO2 | CH4 | 9.6 | 13.3 | 26.4 |  | 2.1 | 41.8 | 32 |
| 1020 | 1 | NiFe-SiO2 | CH4 | 9.5 | 13.6 | 27.0 |  | 2.2 | 42.8 | 32 |
| 1020 | 1 | PdFe-SiO2 | CH4 | 8.0 | 14.4 | 29.3 |  | 2.5 | 46.2 | 32 |
| 1020 | 1 | PtFe-SiO2 | CH4 | 10 | 13.5 | 25.2 |  | 2.1 | 40.8 | 32 |
| 950 | ~ | Fe reactor | CH4/THN | 9 | 7.4 | 28.3 |  | 2.1 | 37.8 | 33 |
| 970 | ~ | Fe reactor | CH4/THN | 11.4 | 8.4 | 26.7 |  | 1.9 | 37.0 | 33 |
| 990 | ~ | Fe reactor | CH4/THN | 13.9 | 9.0 | 24.4 |  | 1.6 | 35.0 | 33 |
| 1010 | ~ | Fe reactor | CH4/THN | 16.5 | 9.8 | 22.4 |  | 1.3 | 33.5 | 33 |
| 1030 | ~ | Fe reactor | CH4/THN | 19.4 | 10.3 | 20.0 |  | 1.1 | 31.4 | 33 |
| 1050 | ~ | Fe reactor | CH4/THN | 25.5 | 9.6 | 16.2 |  | 0.8 | 26.6 | 33 |
| 975 | 6 | / | CH4 | 1.2 | 0 | 0 |  | 3.8 | 3.8 | 34 |
| 975 | 6 | CeO2 | CH4 | 6.9 | 2.4 | 6.7 |  | 2.3 | 11.4 | 34 |
| 975 | 6 | Ptn/CeO2 | CH4 | 9.7 | 6.2 | 8.1 |  | 2.4 | 16.7 | 34 |
| 975 | 6 | Pt1/CeO2 | CH4 | 14.4 | 34.9 | 33.2 |  | 6.6 | 74.7 | 34 |
| 950 | 3.2 | Fe/SiO2a | CH4 | 4.5 | 14.0 | 59.2 |  | 11.6 | 84.8 | 35 |
| 1000 | 3.2 | Fe/SiO2a | CH4 | 13.1 | 15.7 | 43.7 |  | 4.2 | 63.6 | 35 |
| 1050 | 3.2 | Fe/SiO2a | CH4 | 20.5 | 13.9 | 39.7 |  | 3.6 | 57.2 | 35 |
| 1070 | 3.2 | Fe/SiO2a | CH4 | 25.6 | 13.5 | 36.6 |  | 3.4 | 53.5 | 35 |
| 1050 | 3.2 | Fe/SiO2 | CH4 | 14 | 17.6 | 49.4 |  | 4.9 | 71.9 | 35 |
| 1050 | 3.2 | Fe/SiO2 | CH4/H2 | 3.8 | 24.8 | 62.1 |  | 5.7 | 92.6 | 35 |
| 800 | 6 | NiP/SiO2 | CH4 | <0.3 | 0 | 19.4 |  | 38.2 | 57.6 | 36 |
| 900 | 6 | NiP/SiO2 | CH4 | 2.9 | 4.1 | 34.8 |  | 5.3 | 44.2 | 36 |
| 1000 | ~ | Fe/SiO2 | CH4 | 10.5 | 7.2 | 21.6 |  | 1.9 | 30.7 | 37 |

Supplementary Table 3. Inputs and outputs of the calcium carbide (CaC2), partial combustion (PC), thermal plasma, and non-thermal plasma routes per kg of acetylene (C2H2) produced.

| Stream | CaC238 | PC38 | Thermal plasma38,39 | Non-thermal plasma17 |
| --- | --- | --- | --- | --- |
| Feedstock |  |  |  |  |
| Limestone [kg] | 5.00 | - | - | - |
| Coke or biochar [kg] | 2.00 | - | - | - |
| Natural gas or biomethane [kg] | - | 4.46 | 1.55 | 1.48 |
| N-methyl-2-pyrrolidone [kg] | - | 0.01 | 0.01 | - |
| Sodium hypochlorite [kg] | 0.05 | - | - | - |
| Sodium hydroxide [kg] | 1.6E-03 | - | - | - |
| Utilities |  |  |  |  |
| Electricity [kWh] | 10.81 | 3.30 | 12.10* | 12.65 |
| Cooling water [kg] | 12.50 | 3.10 | 6.00 | - |
| Heating – steam [kg] | - | 4.50 | 4.00 | - |
| Emissions to air |  |  |  |  |
| Particulate matter [kg] | 5.1E-04 | 2.5E-04 | 2.3E-04 | - |
| Nitrogen oxides [kg] | 7.8E-04 | 4.8E-04 | 4.5E-04 | - |
| Carbon dioxide [kg] | 3.60 | 0.80 | - | - |
| Volatile organic compounds (VOC) [kg] | 0.32 | - | - | - |
| Non-methane volatile organic compounds (NMVOC) [kg] | - | 3.0E-05 | 3.6E-05 | - |

*The electricity consumption was updated to 12.10 kWh kg–1 C2H2 according to Jiang et al., as the original reference used for the thermal plasma inventory (from Zhang et al.) reported a lower amount than the average range in the literature.

Supplementary Table 4 Inventories used in the life cycle assessment (LCA) to calculate the climate change impact for all acetylene production technologies. The life cycle inventories employed for biomethane were based on premise v2.1.146 sourced from Ecoinvent v3.10, which provides prospective inventories for a range of technologies based on the results derived from the IMAGE Integrated Assessment Model47 under the SSP2 pathway for the year 2020.

| Flow | Activity | Source |
| --- | --- | --- |
| Limestone | market for limestone, unprocessed | Ecoinvent v3.10 |
| Coke | market for coke | Ecoinvent v3.10 |
| Biochar | market for biochar | Peters et al.45 |
| Natural gas | market group for natural gas, high pressure | Ecoinvent v3.10 |
| Biomethane | biomethane production, from biogas upgrading, using amine scrubbing | IMAGE SSP2-RCP6-2020 Ecoinvent v3.10 |
| N-methyl-2-pyrrolidone | market for N-methyl-2-pyrrolidone | Ecoinvent v3.10 |
| Sodium hypochlorite | market for sodium hypochlorite, without water, in 15% solution state | Ecoinvent v3.10 |
| Sodium hydroxide | market for sodium hydroxide, without water, in 50% solution state | Ecoinvent v3.10 |
| Electricity | market group for electricity, high voltage | Ecoinvent v3.10 |
| Cooling water | market for water, deionised | Ecoinvent v3.10 |
| Heating – steam | market for steam, in chemical industry | Ecoinvent v3.10 |

Supplementary Table 5 Cost parameters used are presented in USD (for the year 2022).

| Flow | Value | Ref |
| --- | --- | --- |
| Coke [USD kg–1] | 0.084 | 40 |
| Biochar [USD kg–1] | 0.271 | 41 |
| Methane [USD kg–1] | 0.285 | 42 |
| Biomethane [USD kg–1] | 1.488 | 43 |
| Heating – steam [USD kg–1] | 0.021 | 44 |
| Cooling water [USD kg–1] | 4.8E-05 | 44 |
| Grid electricity [USD kWh–1] | 0.093 | 44 |